Copyright 2010 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 08 14 16 - FLUSH WOOD DOORS

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

      - RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY

        - Section Includes:

          - Solid-core doors withwood-veneer    faces.

Retain one or both subparagraphs below if applicable.  See Evaluations.

        - Related Sections:

Retain Sections in subparagraphs below that contain requirements Contractor might expect to find in this Section but are specified in other Sections.

Retain one of first two options in first subparagraph below, depending on which Section is used to specify wood door frames if used.  Fire-rated and non-fire-rated wood door frames are specified in both Sections.

Retain one of two options in first subparagraph below if any doors are blueprint matched with wood paneling.

          - Section 08 80 00 "Glazing" for glass view panels in flush wood doors.

          - Section 09 91 13 "Exterior Painting"

          - Section 09 91 23 "Interior Painting"

          - Section 09 93 00 "Staining and Transparent Finishing" for field finishing doors.

      - ACTION SUBMITTALS

        - Product Data:  For each type of door indicated.  Include details of core and edge construction and trim for openings.

        - Shop Drawings:  Indicate location, size, and hand of each door; elevation of each kind of door; construction details not covered in Product Data; location and extent of hardware blocking; and other pertinent data.

          - Indicate dimensions and locations of mortises and holes for hardware.

          - Indicate dimensions and locations of cutouts.

          - Indicate requirements for veneer matching.

          - Indicate fire-protection ratings for fire-rated doors.

        - Samples for Verification:

          - Corner sections of doors, approximately 8 by 10 inches (200 by 250 mm), with door faces and edges representing actual materials to be used.

            - Provide samples for each species of veneer and solid lumber required.

          - Frames for light openings, 6 inches (150 mm) long, for each material, type, and finish required.

      - INFORMATIONAL SUBMITTALS

        - Warranty:  Sample of special warranty.

      - QUALITY ASSURANCE

Retain "Manufacturer Qualifications" Paragraph below if required for LEED.  Before retaining, verify that manufacturers comply.  Note that USGBC will allow credit for the full value of the door as certified wood if door manufacturer is listed for chain-of-custody certification and at least 70 percent of wood materials in the door are from certified forests; otherwise, it only allows credit for the value of certified wood materials used in making the door.

        - Manufacturer Qualifications:  A qualified manufacturer that is certified for chain of custody by an FSC-accredited certification body.

Revise first paragraph below or insert exceptions where types of doors specified are not available from a single manufacturer.

        - Source Limitations:  Obtain flush wood doors from single manufacturer.

Retain one standard in first paragraph below.  Verify applicability of selected standard for Project's geographic location.  Review selected standard and coordinate its requirements with selected options.  See Evaluations.

        - Quality Standard:  In addition to requirements specified, comply with AWI's "Architectural Woodwork Quality Standards Illustrated." WDMA I.S.1-A, "Architectural Wood Flush Doors."

Retain first subparagraph below if AWI standard is referenced in paragraph above.  Retain second and third subparagraphs if WI standard is referenced in paragraph above.

          - Provide AWI Quality Certification Labels or an AWI letter of licensing for Project indicating that doors comply with requirements of grades specified.

          - Provide WI-Certified Compliance Certificate indicating that doors comply with requirements of grades specified.

          - Provide WI-Certified Compliance Certificate for installation.

Retain first paragraph below and one of first two options, together with one or more of last five options, if fire-rated doors are required.

        - Fire-Rated Wood Doors:  Doors complying with NFPA 80 that are listed and labeled by a qualified testing agency, for fire-protection ratings indicated, based on testing at [positive pressure] [as close to neutral pressure as possible] according to [NFPA 252] [UBC Standard 7-2] [or] [UL 10B] [UL 10C].

Retain first subparagraph below if applicable and acceptable to authorities having jurisdiction.

          - Oversize Fire-Rated Door Assemblies:  For units exceeding sizes of tested assemblies, provide certification by a qualified testing agency that doors comply with standard construction requirements for tested and labeled fire-rated door assemblies except for size.

Retain subparagraph below if required.  The International Building Code allows an exception for buildings equipped throughout with fire-suppression sprinklers.

          - Temperature-Rise Limit:  [Where indicated] [At vertical exit enclosures and exit passageways], provide doors that have a maximum transmitted temperature end point of not more than 450 deg F (250 deg C) above ambient after 30 minutes of standard fire-test exposure.

Retain paragraph below if Work of this Section is extensive or complex enough to justify a preinstallation conference.

        - Preinstallation Conference:  Conduct conference at [Project site] <Insert location>.

      - DELIVERY, STORAGE, AND HANDLING

        - Comply with requirements of referenced standard and manufacturer's written instructions.

Retain first paragraph below for factory-finished doors and high-quality unfinished doors.  Second option is standard with some manufacturers, extra with others.

        - Package doors individually in [plastic bags or cardboard cartons] [cardboard cartons and wrap bundles of doors in plastic sheeting].

        - Mark each door on[ top and] bottom rail with opening number used on Shop Drawings.

      - PROJECT CONDITIONS

        - Environmental Limitations:  Do not deliver or install doors until spaces are enclosed and weathertight, wet work in spaces is complete and dry, and HVAC system is operating and maintaining ambient temperature and humidity conditions at occupancy levels during the remainder of the construction period.

Generally retain paragraph above; retain paragraph below if humidity will be controlled during occupancy.  If retaining below, retain one of three relative humidity ranges or insert another based on local climatological data.  First option applies to Ontario, Quebec, and most of U.S.  Second applies to damp coastal areas of southern U.S. and the Maritime Provinces.  Third applies to dry southwestern U.S. and to Alberta, Manitoba, and Saskatchewan.  See map and discussion about relative humidity and moisture content in AWI's quality standards.

        - Environmental Limitations:  Do not deliver or install doors until spaces are enclosed and weathertight, wet work in spaces is complete and dry, and HVAC system is operating and maintaining temperature between 60 and 90 deg F (16 and 32 deg C) and relative humidity between [25 and 55] [43 and 70] [17 and 50] <Insert humidity range> percent during the remainder of the construction period.

      - WARRANTY

See Evaluations for door warranties.

When warranties are required, verify with Owner's counsel that special warranties stated in this article are not less than remedies available to Owner under prevailing local laws.

        - Special Warranty:  Manufacturer's standard form in which manufacturer agrees to repair or replace doors that fail in materials or workmanship within specified warranty period.

          - Failures include, but are not limited to, the following:

            - Warping (bow, cup, or twist) more than 1/4 inch (6.4 mm) in a 42-by-84-inch (1067-by-2134-mm) section.

            - Telegraphing of core construction in face veneers exceeding 0.01 inch in a 3-inch (0.25 mm in a 76.2-mm) span.

Requirements in first subparagraph below are not standard with many manufacturers and could be an added cost if retained.

          - Warranty shall also include installation and finishing that may be required due to repair or replacement of defective doors.

Warranties for exterior doors vary from no warranty to a warranty for a period of up to five years.  Before retaining first subparagraph below, verify availability of warranty period with manufacturers selected; delete if retaining manufacturers that offer no warranty.  Standard manufacturer's warranty generally goes into effect on date of shipment, not date of Substantial Completion.

          - Warranty Period for Solid-Core Exterior Doors:  [Two] [Five] <Insert number> years from date of Substantial Completion.

First subparagraph below is typical; revise if required.

          - Warranty Period for Solid-Core Interior Doors:  Life of installation.

Warranties for hollow-core doors vary with manufacturer and type of hollow core.  Before retaining subparagraph below, verify availability of warranty period with manufacturers selected.  Standard manufacturer's warranties generally go into effect on date of shipment, not date of Substantial Completion.

          - Warranty Period for Hollow-Core Interior Doors:  [One] [Two] <Insert number> year(s) from date of Substantial Completion.

- PRODUCTS

      - MANUFACTURERS

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers.  Retain paragraph and list of manufacturers in this article.  See Section 016000 "Product Requirements."

        - Manufacturers:  Subject to compliance with requirements, provide products by one of the following :

Manufacturers listed are representative only; many others make flush wood doors.  See WDMA's and AWI's Web sites for listings of door manufacturers.  Retain only manufacturers offering doors complying with requirements selected for each type used, and add other manufacturers offering suitable products.  See Evaluations and manufacturers' catalogs.

          - Eggers Industries

          - VT Industries Inc.

          - Substitutions:  See Section 01 25 00 - Substitution Procedures.

      - DOOR CONSTRUCTION, GENERAL

Retain "Certified Wood" Paragraph below if required for LEED.  An alternative method of dealing with this credit requirement is to retain requirement in Section 018113.13 "Sustainable Design Requirements - LEED for New Construction and Major Renovations," Section 018113.16 "Sustainable Design Requirements - LEED for Commercial Interiors," Section 018113.19 "Sustainable Design Requirements - LEED for Core and Shell Development," and Section 018113.23 "Sustainable Design Requirements - LEED for Schools" that gives Contractor the option and responsibility to determine how the credit requirement will be met.

        - Certified Wood:  Fabricate doors with [cores] [veneers] [not less than 70 percent of wood products] [all wood products] produced from wood obtained from forests certified by an FSC-accredited certification body to comply with FSC STD-01-001, "FSC Principles and Criteria for Forest Stewardship."

Retain "Low-Emitting Materials" Paragraph below if required for LEED-NC, LEED-CS, or LEED-CI Credit IEQ 4.4.  Before retaining, verify availability with manufacturers.

        - Low-Emitting Materials:  Fabricate doors with adhesives and composite wood products that do not contain urea formaldehyde.

Retain "Low-Emitting Materials" Paragraph below if required for LEED for Schools Credit IEQ 4.

        - Low-Emitting Materials:  Fabricate doors with [adhesives] [and] [composite wood products] that comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

Retain one of first two paragraphs below to specify performance grade if WDMA I.S.1-A is referenced, or delete both paragraphs and specify performance grades for each door type in "Veneer-Faced Doors for Transparent Finish," "Doors for Opaque Finish," and "Plastic-Laminate-Faced Doors" articles.  See Evaluations.

        - WDMA I.S.1-A Performance Grade:  [Extra Heavy Duty] [Heavy Duty] [Standard Duty] [As indicated].

        - WDMA I.S.1-A Performance Grade:

          - Heavy Duty unless otherwise indicated.

          - Extra Heavy Duty:  [Classrooms] [public toilets] [janitor's closets] [assembly spaces] [exits] [patient rooms] <Insert locations> [and where indicated].

          - Standard Duty:  [Closets (not including janitor's closets)] [private toilets] <Insert locations> [and where indicated].

        - Structural-Composite-Lumber-Core Doors:

          - Structural Composite Lumber:  WDMA I.S.10.

            - Screw Withdrawal, Face:  700 lbf (3100 N).

            - Screw Withdrawal, Edge:  400 lbf (1780 N).

        - Fire-Protection-Rated Doors:  Provide core specified or mineral core as needed to provide fire-protection rating indicated.

Edge construction in first subparagraph below is used when positive-pressure fire testing is required; surface-applied intumescent seals can also be used.

          - Edge Construction:  Provide edge construction with intumescent seals concealed by outer stile.  Comply with specified requirements for exposed edges.

Retain first subparagraph below if steel edges and astragals are not acceptable.  Coordinate availability and ratings with manufacturers selected.  Retain option if positive-pressure fire testing is required.

          - Pairs:  Provide fire-retardant stiles that are listed and labeled for applications indicated without formed-steel edges and astragals.[  Provide stiles with concealed intumescent seals.] Comply with specified requirements for exposed edges.

Retain first subparagraph below if steel edges and astragals are acceptable.  Retain option if positive-pressure fire testing is required.

          - Pairs:  Provide formed-steel edges and astragals[ with intumescent seals].

            - Finish steel edges and astragals with baked enamel[ same color as doors].

Retain subparagraph above or below; delete option above if edges and astragals will be field painted.

            - Finish steel edges and astragals to match door hardware (locksets or exit devices).

        - Mineral-Core Doors:

          - Core:  Noncombustible mineral product complying with requirements of referenced quality standard and testing and inspecting agency for fire-protection rating indicated.

          - Blocking:  Provide composite blocking with improved screw-holding capability approved for use in doors of fire-protection ratings indicated  as follows:

Retain "Blocking" Subparagraph above and first four subparagraphs below only after verifying availability for fire-protection rating required.  Delete four subparagraphs below if retaining first option above.

            - 5-inch (125-mm) top-rail blocking.

            - 5-inch (125-mm) bottom-rail blocking, in doors indicated to have protection plates.

            - 5-inch (125-mm) midrail blocking, in doors indicated to have armor plates.

            - 5-inch (125-mm) midrail blocking, in doors indicated to have exit devices.

          - Edge Construction:  At hinge stiles, provide laminated-edge construction with improved screw-holding capability and split resistance.  Comply with specified requirements for exposed edges.

      - VENEERED-FACED DOORS FOR TRANSPARENT FINISH

        - Exterior Solid-Core Doors <Insert drawing designation>:

Grade AA faces are required for AWI and WI Premium grade doors; Grade A faces are required for WDMA I.S.1-A Premium grade doors.  See Evaluations.  WDMA and WI have no Economy grade for doors.

          - Grade:  [Premium, with Grade AA faces] [Premium, with Grade A faces] [Custom (Grade A faces)] [Economy (Grade B faces)].

Options in first subparagraph below are examples only; revise or insert another species.  Last two options are examples of tropical species available as FSC-certified veneers (available from ForestWorld Group).

          - Species:  [Anigre] [Select white ash] [Figured select white ash] [Select white birch] [Cherry] [Select red gum] [Figured select red gum] [Select white maple] [Red oak] [Persimmon] [Sapele] [Sycamore] [Walnut] [White oak] [Ucuuba (Virola Duckei)] [Cupiuba (Goupia glabra)] <Insert species>.

Option for rift cut in first subparagraph below applies only to oak.

          - Cut:  [Rotary cut] [Plain sliced (flat sliced)] [Quarter sliced] [Rift cut].

Pleasing match in first subparagraph below is available only for Economy grade doors (Grade B faces).  See Evaluations.

          - Match between Veneer Leaves:  [Book] [Slip] [Pleasing] match.

Center-balance match in first subparagraph below is expensive and is not standard with any grade of door.  Balance match is required for AWI and WI Premium grade doors.  Running match is standard for Custom grade and WDMA Premium grade doors.  See Evaluations.

          - Assembly of Veneer Leaves on Door Faces:  [Center-balance] [Balance] [Running] match.

          - Pair and Set Match:  Provide for doors hung in same opening[ or separated only by mullions].

Retain first option in first subparagraph below if top edges of doors will be visible, such as doors in multistory spaces.  Retain one of four remaining options; last two require factory prefitting.

          - Exposed Vertical[ and Top] Edges:  [Same species as faces or a compatible species] [Same species as faces] [Applied wood-veneer edges of same species as faces and covering edges of faces] [Applied wood edges of same species as faces and covering edges of crossbands].

Particleboard cores in first subparagraph below are not generally recommended for exterior doors.

          - Core:  [Particleboard] [Glued wood stave] [Structural composite lumber] [Either glued wood stave or structural composite lumber].

Retain one of four options in subparagraph above and one of first two options in first subparagraph below.  Third option below applies to some five-ply doors.

          - Construction:  [Five] [Five or seven] plies.  Stiles and rails are bonded to core, then entire unit abrasive planed before veneering.[  Faces are bonded to core using a hot press.]

          - Adhesives:  Type I per WDMA TM-6.

WDMA indicates that its standard is not intended for exterior doors.  If exterior flush wood doors are required and WDMA I.S.1-A is referenced, usually retain first option in subparagraph below.  Delete subparagraph if performance grades are specified in "Door Construction, General" Article.

          - WDMA I.S.1-A Performance Grade:  [Extra Heavy] [Heavy] Duty.

        - Interior Solid-Core Doors <Insert drawing designation>:

Grade AA faces are required for AWI and WI Premium grade doors; Grade A faces are required for WDMA I.S.1-A Premium grade doors.  See Evaluations.  WDMA and WI have no Economy grade for doors.

          - Grade:  [Premium, with Grade AA faces] [Premium, with Grade A faces] [Custom (Grade A faces)] [Economy (Grade B faces)].

Options in first subparagraph below are examples only; revise or insert another species.  Last two options are examples of tropical species available as FSC-certified veneers (available from ForestWorld Group).

          - Species:  [Anigre] [Select white ash] [Figured select white ash] [Select white birch] [Cherry] [Select red gum] [Figured select red gum] [Select white maple] [Red oak] [Persimmon] [Sapele] [Sycamore] [Walnut] [White oak] [Ucuuba (Virola Duckei)] [Cupiuba (Goupia glabra)] <Insert species>.

Option for rift cut in first subparagraph below applies only to oak.

          - Cut:  [Rotary cut] [Plain sliced (flat sliced)] [Quarter sliced] [Rift cut].

Pleasing match in first subparagraph below is available only for Economy grade doors (Grade B faces).  See Evaluations.

          - Match between Veneer Leaves:  [Book] [Slip] [Pleasing] match.

Center-balance match in first subparagraph below is expensive and is not standard with any grade of door.  Balance match is required for AWI and WI Premium grade doors.  Running match is standard for Custom grade and WDMA Premium grade doors.  See Evaluations.

          - Assembly of Veneer Leaves on Door Faces:  [Center-balance] [Balance] [Running] match.

          - Pair and Set Match:  Provide for doors hung in same opening[ or separated only by mullions].

          - Room Match:  Match door faces within each separate room or area of building.  Corridor-door faces do not need to match where they are separated by [10 feet (3 m)] [20 feet (6 m)] <Insert distance> or more.

Retain subparagraph above or first subparagraph below only for highest quality work with Premium grade doors.  Below is based on requirement for WI Premium grade doors.

          - Room Match:  Provide door faces of compatible color and grain within each separate room or area of building.

Before retaining first subparagraph below, verify availability of veneers for selected matching; usually retain first option.  See referenced standards.

          - Transom Match:  [Continuous match] [End match] [As indicated].

          - Blueprint Match:  Where indicated, provide doors with faces produced from same flitches as adjacent wood paneling and arranged to provide blueprint match with wood paneling.  Comply with requirements in [Section 06 40 23 "Interior Architectural Woodwork."] [Section 06 42 00 "Wood Paneling."]

Retain first option in first subparagraph below if top edges of doors will be visible, such as doors in multistory spaces.  Retain one of four remaining options; last two require factory prefitting.

          - Exposed Vertical[ and Top] Edges:  [Same species as faces or a compatible species] [Same species as faces] [Applied wood-veneer edges of same species as faces and covering edges of faces] [Applied wood edges of same species as faces and covering edges of crossbands].

Retain one of five options in first subparagraph below.

          - Core:  [Particleboard] [Glued wood stave] [Structural composite lumber] [Either glued wood stave or structural composite lumber] [Either glued or nonglued wood stave or structural composite lumber].

          - Construction:  [Five] [Five or seven] plies.  Stiles and rails are bonded to core, then entire unit abrasive planed before veneering.[  Faces are bonded to core using a hot press.]

Retain one of first two options in subparagraph above or retain first subparagraph below.  Third option above applies to some five-ply doors.  Glued-wood-stave core is only available with bonded construction and nonglued-wood-stave core is only available with nonbonded construction.

          - Construction:  Seven plies, either bonded or nonbonded construction.

Delete subparagraph below if WDMA I.S.1-A is not referenced or if performance grades are specified in "Door Construction, General" Article.

          - WDMA I.S.1-A Performance Grade:  [Extra Heavy Duty] [Heavy Duty] [Standard Duty] [As indicated].

      - DOORS FOR OPAQUE FINISH

        - Exterior Solid-Core Doors <Insert drawing designation>:

WDMA and WI have no Economy grade for doors.

          - Grade:  [Premium] [Custom] [Economy].

First option in first subparagraph below is highest quality.  Coordinate with requirements of door grade selected.

          - Faces:  [Medium-density overlay] [Any closed-grain hardwood of mill option].

            - Apply medium-density overlay to [standard-thickness, closed-grain, hardwood face veneers] [or] [directly to high-density hardboard crossbands].

Retain option in first subparagraph below if top edges of doors will be visible, such as doors in multistory spaces.

          - Exposed Vertical[ and Top] Edges:  Any closed-grain hardwood.

Particleboard cores in first subparagraph below are not generally recommended for exterior doors.

          - Core:  [Particleboard] [Glued wood stave] [Structural composite lumber] [Either glued wood stave or structural composite lumber].

Retain one of four options in subparagraph above and one of first two options in first subparagraph below.  Third option below applies to some five-ply doors.

          - Construction:  [Five] [Five or seven] plies.  Stiles and rails are bonded to core, then entire unit abrasive planed before veneering.[  Faces are bonded to core using a hot press.]

          - Adhesives:  Type I per WDMA TM-6.

WDMA indicates that its standard is not intended for exterior doors.  If exterior flush wood doors are required and WDMA I.S.1-A is referenced, usually retain first option in subparagraph below.  Delete subparagraph if performance grades are specified in "Door Construction, General" Article.

          - WDMA I.S.1-A Performance Grade:  [Extra Heavy] [Heavy] Duty.

        - Interior Solid-Core Doors <Insert drawing designation>:

WDMA and WI have no Economy grade for doors.

          - Grade:  [Premium] [Custom] [Economy].

First option in first subparagraph below is highest quality; last is most economical.  Coordinate with requirements of door grade selected.

          - Faces:  [Medium-density overlay] [Any closed-grain hardwood of mill option] [Hardboard or MDF].

            - Apply medium-density overlay to [standard-thickness, closed-grain, hardwood face veneers] [or] [directly to high-density hardboard crossbands].

            - Hardboard Faces:  AHA A135.4, Class 1 (tempered) or Class 2 (standard).

            - MDF Faces:  ANSI A208.2, Grade 150 or 160.

Retain option in first subparagraph below if top edges of doors will be visible, such as doors in multistory spaces.

          - Exposed Vertical[ and Top] Edges:  Any closed-grain hardwood.

Retain one of five options in first subparagraph below.

          - Core:  [Particleboard] [Glued wood stave] [Structural composite lumber] [Either glued wood stave or structural composite lumber] [Either glued or nonglued wood stave or structural composite lumber].

          - Construction:  [Three] [Five] [Five or seven] plies.  Stiles and rails are bonded to core, then entire unit abrasive planed before veneering.[  Faces are bonded to core using a hot press.]

Retain one of first three options in subparagraph above or retain first subparagraph below.  Fourth option above applies to some five-ply doors.  Glued-wood-stave core is only available with bonded construction and nonglued-wood-stave core is only available with nonbonded construction.  Retain first option in either subparagraph for hardboard.  Three-ply construction applies to doors with hardboard or MDF faces.

          - Construction:  [Three] [Seven] plies, either bonded or nonbonded construction.

Delete subparagraph below if WDMA I.S.1-A is not referenced or if performance grades are specified in "Door Construction, General" Article.

          - WDMA I.S.1-A Performance Grade:  [Extra Heavy Duty] [Heavy Duty] [Standard Duty] [As indicated].

      - LOUVERS

        - Wood Louvers:  Door manufacturer's standard solid-wood louvers unless otherwise indicated.

Retain one of three species in subparagraph below.

          - Wood Species:  [Same species as door faces] [Species compatible with door faces] [Any closed-grain hardwood].

Retain one or more of three paragraphs below if light openings are required.

        - Wood Beads for Light Openings in Wood Doors:  Provide manufacturer's standard wood beads as follows unless otherwise indicated.

Retain one of three wood species in first subparagraph below.

          - Wood Species:  Same species as door faces  .

Retain one of five options in first subparagraph below or revise to suit Project.

          - Profile:  [Flush rectangular beads] [Recessed tapered beads] [Recessed tapered beads with exposed banding] [Lipped tapered beads] [Manufacturer's standard shape].

Retain subparagraph below if required.

          - At wood-core doors with 20-minute fire-protection ratings, provide wood beads and metal glazing clips approved for such use.

Retain one of two paragraphs below if required for doors with fire-protection rating exceeding 20 minutes.

        - Wood-Veneered Beads for Light Openings in Fire-Rated Doors:  Manufacturer's standard wood-veneered noncombustible beads matching veneer species of door faces and approved for use in doors of fire-protection rating indicated.  Include concealed metal glazing clips where required for opening size and fire-protection rating indicated.

        - Metal Frames for Light Openings in Fire-Rated Doors:  Manufacturer's standard frame formed of 0.048-inch- (1.2-mm-) thick, cold-rolled steel sheet; factory primed for paint finish ; and approved for use in doors of fire-protection rating indicated.

      - FABRICATION

Delete first paragraph below if no doors are required to be factory fitted.  Retain paragraph and revise to indicate exceptions if only some doors are required to be factory fitted.  Plastic-laminate-edged and factory-finished doors must be factory fitted and machined.  Fire-rated and plastic-laminate-faced doors with wood edges should also be factory fitted and machined.  Factory fitting and machining for other doors are optional.  See Evaluations.

Standard fitting may be inadequate for doors 2-1/2 inches (64 mm) thick or more or for doors exposed to wide changes in humidity and temperature.

        - Factory fit doors to suit frame-opening sizes indicated.  Comply with clearance requirements of referenced quality standard for fitting unless otherwise indicated.

          - Comply with requirements in NFPA 80 for fire-rated doors.

Delete first paragraph below if no doors are required to be factory machined.  Retain paragraph and revise to indicate exceptions if only some doors are required to be factory machined.  See Evaluations.

        - Factory machine doors for hardware that is not surface applied.  Locate hardware to comply with DHI-WDHS-3.  Comply with final hardware schedules, door frame Shop Drawings, DHI A115-W series standards, and hardware templates.

Retain first subparagraph below for metal frames for wood doors.

          - Coordinate with hardware mortises in metal frames to verify dimensions and alignment before factory machining.

Retain subparagraph below with pairs of factory-fitted, fire-rated doors where astragals, etc., are required.

          - Metal Astragals:  Factory machine astragals and formed-steel edges for hardware for pairs of fire-rated doors.

Retain first paragraph below if applicable.  Indicate here or on Drawings if doors and transoms are rabbeted.  Verify that transom sizes and attachment methods comply with fire-protection ratings if fire-rated doors with transoms are used.

        - Transom and Side Panels:  Fabricate matching panels with same construction, exposed surfaces, and finish as specified for associated doors.  Finish bottom edges of transoms and top edges of rabbeted doors same as door stiles.

Retain subparagraph below if applicable or revise if another method of attachment is required.

          - Fabricate door and transom panels with full-width, solid-lumber, rabbeted, meeting rails.  Provide factory-installed spring bolts for concealed attachment into jambs of metal door frames.

        - Openings:  Cut and trim openings through doors in factory.

          - Light Openings:  Trim openings with moldings of material and profile indicated.

First subparagraph below is unnecessary if only metal light frames are used.

          - Glazing:  Factory install glazing in doors indicated to be factory finished.  Comply with applicable requirements in Section 08 80 00 "Glazing."

Usually retain paragraph below to provide additional weather resistance.

        - Exterior Doors:  Factory treat exterior doors with water repellent after fabrication has been completed but before [shop priming] [factory finishing].

Retain subparagraph below for outswinging exterior doors.  Before retaining, verify availability with manufacturers selected or delete and include with weather stripping in Section 087100 "Door Hardware" and Section 087111 "Door Hardware (Descriptive Specification)" Flash top of outswinging doors (with manufacturer's standard metal flashing).

      - SHOP PRIMING

Retain this article if factory-finished doors are not required.  Factory fitting is recommended to minimize damage to shop-primed doors.

        - Doors for Opaque Finish:  Shop prime doors with one coat of wood primer specified in Section 09 91 13 "Exterior Painting." Section 09 91 23 "Interior Painting." Seal all four edges, edges of cutouts, and mortises with primer.

Retain paragraph above or below, or both, as applicable.

        - Doors for Transparent Finish:  Shop prime doors with stain (if required), other required pretreatments, and first coat of finish as specified in   Section 09 93 00 "Staining and Transparent Finishing." Seal all four edges, edges of cutouts, and mortises with first coat of finish.

- EXECUTION

      - EXAMINATION

        - Examine doors and installed door frames before hanging doors.

          - Verify that frames comply with indicated requirements for type, size, location, and swing characteristics and have been installed with level heads and plumb jambs.

          - Reject doors with defects.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

      - INSTALLATION

        - Hardware:  For installation, see Section 08 71 00 "Door Hardware" and Section 08 71 11 "Door Hardware (Descriptive Specification)."

        - Installation Instructions:  Install doors to comply with manufacturer's written instructions and the referenced quality standard, and as indicated.

Retain subparagraph below for fire-rated doors.

          - Install fire-rated doors in corresponding fire-rated frames according to NFPA 80.

Retain first paragraph below if all doors are not factory fitted.  Factory fitting of fire-rated doors is preferred to job fitting because of limitations on trimming narrower stiles and rails.

        - Job-Fitted Doors:  Align and fit doors in frames with uniform clearances and bevels as indicated below; do not trim stiles and rails in excess of limits set by manufacturer or permitted for fire-rated doors.  Machine doors for hardware.  Seal edges of doors, edges of cutouts, and mortises after fitting and machining.

          - Clearances:  Provide 1/8 inch (3.2 mm) at heads, jambs, and between pairs of doors.  Provide 1/8 inch (3.2 mm) from bottom of door to top of decorative floor finish or covering unless otherwise indicated.  Where threshold is shown or scheduled, provide 1/4 inch (6.4 mm) from bottom of door to top of threshold unless otherwise indicated.

Retain first subparagraph below for fire-rated doors or if doors are not factory fitted.

            - Comply with NFPA 80 for fire-rated doors.

          - Bevel non-fire-rated doors 1/8 inch in 2 inches (3-1/2 degrees) at lock and hinge edges.

Subparagraph above is standard bevel; revise to suit Project if required.  See Evaluations.  Retain subparagraph below for fire-rated doors or if doors are not factory fitted.  Fire-rated doors can be trimmed only to a limited extent because of narrow stiles and rails.

          - Bevel fire-rated doors 1/8 inch in 2 inches (3-1/2 degrees) at lock edge; trim stiles and rails only to extent permitted by labeling agency.

        - Factory-Fitted Doors:  Align in frames for uniform clearance at each edge.

        - Factory-Finished Doors:  Restore finish before installation if fitting or machining is required at Project site.

      - ADJUSTING

        - Operation:  Rehang or replace doors that do not swing or operate freely.

        - Finished Doors:  Replace doors that are damaged or that do not comply with requirements.  Doors may be repaired or refinished if work complies with requirements and shows no evidence of repair or refinishing.

END OF SECTION 08 14 16