Copyright 2010 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 09 65 16 - RESILIENT SHEET FLOORING

- GENERAL

      - RELATED DOCUMENTS

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY

        - Section Includes:

          - Vinyl sheet floor covering, [with] [and] [without] backing.

          - Rubber sheet floor covering, [with] [and] [without] backing.

        - Related Sections:

Retain Sections in subparagraphs below that contain requirements Contractor might expect to find in this Section but are specified in other Sections.

          - Section 09 65 13 "Resilient Base and Accessories" for resilient base, reducer strips, and other accessories installed with resilient floor coverings.

          - Section 09 65 19 "Resilient Tile Flooring" for resilient floor tile.

      - ACTION SUBMITTALS

        - Product Data:  For each type of product indicated.

        - LEED Submittals (Projects authorized for LEED certification only):

"Product Data for Credit IEQ 4.1" Subparagraph below applies to LEED-NC, LEED-CI, and LEED-CS; coordinate with requirements selected in Part 2 for adhesives and chemical-bonding compounds.

          - Product Data for Credit IEQ 4.1:  For [adhesives] [and] [chemical-bonding compounds], documentation including printed statement of VOC content.

"Product Data for Credit IEQ 4.3" Subparagraph below applies to LEED-NC, LEED-CI, and LEED-CS; coordinate with requirements selected in Part 2 for adhesives and chemical-bonding compounds.

          - Product Data for Credit IEQ 4.3:  For adhesives [and chemical-bonding compounds], documentation including printed statement of VOC content.

"Product Data for Credit IEQ 4.3" Subparagraph below applies to LEED-NC, LEED-CI, and LEED-CS; coordinate with requirements selected in Part 2 for resilient sheet flooring.

          - Product Data for Credit IEQ 4.3:  For resilient sheet flooring, documentation from an independent testing agency indicating compliance with the FloorScore Standard.

"Laboratory Test Reports for Credit IEQ 4" Subparagraph below applies to LEED for Schools.

          - Laboratory Test Reports for Credit IEQ 4:  For adhesives [flooring system] [and] [chemical-bonding compounds], documentation indicating that products comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

Retain first paragraph below if required.

        - Shop Drawings:  For each type of floor covering.  Include floor covering layouts, locations of seams, edges, columns, doorways, enclosing partitions, built-in furniture, cabinets, and cutouts.

          - Show details of special patterns.

        - Samples for Initial Selection:  For each type of floor covering indicated.

Delete "Samples for Initial Selection" Paragraph above if colors and other characteristics are preselected and specified or scheduled.  Retain first paragraph below with or without above.

        - Samples for Verification:  In manufacturer's standard size, but not less than [6-by-9-inch (150-by-230-mm)] <Insert size> sections of each different color and pattern of floor covering required.

          - For heat-welding bead, manufacturer's standard-size Samples, but not less than [9 inches (230 mm)] <Insert dimension> long, of each color required.

Floor covering is usually specified for seamless installation.  Retain first paragraph below for heat-welded or chemically-bonded seams.

        - Seam Samples:  For seamless-installation technique indicated and for each floor covering product, color, and pattern required; with seam running lengthwise and in center of [6-by-9-inch (150-by-230-mm)] <Insert size> Sample applied to a rigid backing and prepared by Installer for this Project.

        - Product Schedule:  For floor coverings.[  Use same designations indicated on Drawings.]

      - INFORMATIONAL SUBMITTALS

Coordinate first paragraph below with qualification requirements in Section 014000 "Quality Requirements" and as supplemented in "Quality Assurance" Article.

        - Qualification Data:  For qualified Installer.

      - CLOSEOUT SUBMITTALS

        - Maintenance Data:  For each type of floor covering to include in maintenance manuals.

      - MAINTENANCE MATERIAL SUBMITTALS

        - Furnish extra materials that match products installed and that are packaged with protective covering for storage and identified with labels describing contents.

Revise subparagraph below to suit Project.

          - Floor Covering:  Furnish quantity not less than [10 linear feet (3 linear m)] <Insert length> for every [500 linear feet (150 linear m)] <Insert length> or fraction thereof, in roll form and in full roll width for each color, pattern, and type of floor covering installed.

      - QUALITY ASSURANCE

Retain option in first paragraph below for heat-welded or chemically bonded seams.

        - Installer Qualifications:  A qualified installer who employs workers for this Project who are competent in techniques required by manufacturer for floor covering installation [and seaming method] indicated.

Not all manufacturers train or certify installers.  Before retaining subparagraph below, verify availability with manufacturers selected; retain with "Qualification Data" Paragraph in "Informational Submittals" Article.

          - Engage an installer who employs workers for this Project who are trained or certified by floor covering manufacturer for installation techniques required.

Delete first paragraph below if fire-test-response testing is not required by authorities having jurisdiction.  In most building codes, resilient floor coverings are exempt from fire-test-response requirements.  See "Fire-Test-Response Characteristics" Article in the Evaluations in Section 096500 "Resilient Flooring" for additional information.

        - Fire-Test-Response Characteristics:  As determined by testing identical products according to ASTM E 648 or NFPA 253 by a qualified testing agency.

          - Critical Radiant Flux Classification:  Class I, not less than 0.45 W/sq. cm.

        - Mockups:  Build mockups to verify selections made under sample submittals and to demonstrate aesthetic effects and set quality standards for materials and execution.

          - Build mockups for floor coverings including[ resilient base and] accessories.

            - Size:  Minimum 100 sq. ft. (9.3 sq. m) for each type, color and pattern [in locations indicated] [in locations directed by Architect] <Insert location requirements>.

      - DELIVERY, STORAGE, AND HANDLING

        - Store floor coverings and installation materials in dry spaces protected from the weather, with ambient temperatures maintained within range recommended by manufacturer, but not less than 50 deg F (10 deg C) or more than 90 deg F (32 deg C).  Store rolls upright.

      - PROJECT CONDITIONS

Ambient temperature range for installation varies among manufacturers.  Consult manufacturers for recommendations and revise first paragraph below to suit Project.

        - Maintain ambient temperatures within range recommended by manufacturer, but not less than [70 deg F (21 deg C)] <Insert temperature> or more than [85 deg F (29 deg C)] <Insert temperature>, in spaces to receive floor coverings during the following time periods:

          - 48 hours before installation.

          - During installation.

          - 48 hours after installation.

        - Until Substantial Completion, maintain ambient temperatures within range recommended by manufacturer, but not less than [55 deg F (13 deg C)] <Insert temperature> or more than [95 deg F (35 deg C)] <Insert temperature>.

        - Close spaces to traffic during floor covering installation.

        - Close spaces to traffic for 48 hours after floor covering installation.

        - Install floor coverings after other finishing operations, including painting, have been completed.

- PRODUCTS

      - PERFORMANCE REQUIREMENTS

Retain first paragraph below if required for LEED-NC, LEED-CS, or LEED-CI Credit IEQ 4.3; before retaining, verify availability of materials that comply.

        - FloorScore Compliance:  Resilient sheet flooring shall comply with requirements of FloorScore Standard.

Retain "Low-Emitting Materials" Paragraph below if required for LEED for Schools Credit IEQ 4.

        - Low-Emitting Materials:  Flooring system shall comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

      - VINYL SHEET FLOOR COVERING

Copy this article and re-edit for each product.

Insert number to complete drawing designation.  Use these designations on Drawings to identify each product.

See Editing Instruction No. 1 in the Evaluations in Section 096500 "Resilient Flooring" for cautions about naming manufacturers and products.  See Section 016000 "Product Requirements."

        - Products:  Subject to compliance with requirements,  provide one of the following :

          - Armstrong World Industries, Inc.; <Medintech>.

          - Forbo Flooring, Inc.; Forza.

          - Tarkett, Inc.; Aria.

          - Substitute:  see section 01 25 00 – Substitution Procedures.

Retain paragraph above or first paragraph below to suit products selected.

        - Vinyl Sheet Floor Covering with Backing:  ASTM F 1303.

          - Type (Binder Content):   Type II, minimum binder content of 34 percent.

          - Wear-Layer Thickness:  Grade 1.

          - Overall Thickness:   1/8 inch minimum.

          - Backing Class:  Class A (fibrous)  .

        - Wearing Surface:  Color and pattern throughout   .

        - Sheet Width:  As standard with manufacturer      .

Revise first paragraph below to suit Project.  Generally, manufacturers prefer the appearance and performance of seamless installations.  See "General Comments" Article in the Evaluations in Section 096500 "Resilient Flooring" for a discussion of seamless installation techniques.

        - Seaming Method:  Heat welded, solid vinyl bead, in color matching field color   .

Retain paragraph below if colors and patterns are not indicated in a separate schedule.

        - Colors and Patterns:    As selected by Architect from full range of industry colors.

      - RUBBER SHEET FLOOR COVERING

Copy this article and re-edit for each product.

Insert number to complete drawing designation.  Use these designations on Drawings to identify each product.

See Editing Instruction No. 1 in the Evaluations in Section 096500 "Resilient Flooring" for cautions about naming manufacturers and products.  See Section 016000 "Product Requirements."

        - Products:  Subject to compliance with requirements,  provide one of the following :

          - Johnsonite; Rondel Speckled.

          - PRF USA Inc.; Activa.

          - R.C.A. Rubber Company (The); Flexi Flor.

          - Substitute:  see section 01 25 00 – Substitution Procedures.

Retain paragraph above or first paragraph below to suit products selected.

        - Rubber Sheet Floor Covering with Backing:  ASTM F 1860.

          - Type:  Type I, homogeneous rubber sheet with backing .

          - Wear-Layer Thickness:  As standard with manufacturer .

For molded-pattern (raised-pattern) rubber sheet, overall thickness is generally measured at the thickest cross-sectional area of flooring product.

          - Overall Thickness:   1/8 inch minimum.

Retain and revise first subparagraph below for Type II, layered rubber sheet with backing.

          - Backing Type:  Fibrous) .

See "Rubber Sheet Floor Coverings" Article in the Evaluations in Section 096500 "Resilient Flooring" for a discussion of hardness values.

        - Hardness:   Not less than required by ASTM F 1860 .

        - Wearing Surface:    Color and pattern throughout.

          - Molded-Pattern Figure:  Raised discs  .

        - Sheet Width:  As standard with manufacturer      .

Revise first paragraph below to suit Project.  Generally, manufacturers prefer the appearance and performance of seamless installations.  See "General Comments" Article in the Evaluations in Section 096500 "Resilient Flooring" for a discussion of seamless installation techniques.

        - Seaming Method:  Heat welded   .

Retain paragraph below if colors and patterns are not indicated in a separate schedule.

        - Colors and Patterns:    As selected by Architect from full range of industry colors.

      - RESILIENT BASE

        - Resilient Base:  ASTM F 1861, Type TS rubber, vulcanized thermoset; top set style cove, and as follows:

          - Height:  4 inch.

          - Thickness:  0.125 inch thick.

          - Finish:  Matte.

          - Length:  Roll

          - Color:  Black, unless otherwise indicated.

          - Accessories:  Premolded external corners and end stops.

          - Manufacturers:

            - Johnsonite, Inc:  www.johnsonite.com.

            - Roppe Corp:  www.roppe.com.

            - Substitutions:  See Section 01 60 00 – Product Requirements.

      - INSTALLATION MATERIALS

        - Trowelable Leveling and Patching Compounds:  Latex-modified, portland cement based or blended hydraulic-cement-based formulation provided or approved by manufacturer for applications indicated.

        - Adhesives:  Water-resistant type recommended by manufacturer to suit floor covering and substrate conditions indicated.

Retain first subparagraph below if required for LEED-NC, LEED-CI, or LEED-CS Credit IEQ 4.1 or Credit IEQ 4.3.  First option is VOC content limit for VCT and asphalt tile adhesives; second is that for rubber floor adhesives.

          - Adhesives shall have a VOC content of not more than 50   g/L when calculated according to 40 CFR 59, Subpart D (EPA Method 24).

Retain subparagraph below if required for LEED for Schools Credit IEQ 4.

          - Adhesives shall comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

        - Seamless-Installation Accessories:

          - Heat-Welding Bead:  Manufacturer's solid-strand product for heat welding seams.

            - Color:   Match floor field covering .

          - Chemical-Bonding Compound:  Manufacturer's product for chemically bonding seams.

Retain first subparagraph below if required for LEED-NC, LEED-CI, or LEED-CS Credit IEQ 4.1 Credit IEQ 4.1 or Credit IEQ 4.3.  VOC content limit is that for PVC welding compounds; LEED does not include a limit for rubber welding compounds.

            - VOC Content:  Not more than 510 g/L. when calculated according to 40 CFR 59, Subpart D (EPA Method 24).

Retain subparagraph below if required for LEED for Schools Credit IEQ 4.

            - Bonding compound shall comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

        - Integral-Flash-Cove-Base Accessories:

          - Cove Strip:  1-inch (25-mm) radius provided or approved by manufacturer.

          - Cap Strip:  Square metal, vinyl, or rubber cap   provided or approved by manufacturer.

Not all manufacturers' written installation instructions require metal inside and outside corners.  Delete subparagraph below if not applicable.

          - Corners:  Metal inside and outside corners and end stops provided or approved by manufacturer.

Retain paragraph below for use with most sheet vinyl floor coverings.  Liquid floor polish is generally used instead of paste wax.  See "Maintenance Procedures" Article in the Evaluations in Section 096500 "Resilient Flooring" for additional information.

        - Floor Polish:  Provide protective liquid floor polish products as recommended by manufacturer.

- EXECUTION

      - EXAMINATION

Coordinate requirements specified in other Sections for subfloor construction and tolerances to ensure that they are appropriate for floor coverings selected.

        - Examine substrates, with Installer present, for compliance with requirements for maximum moisture content and other conditions affecting performance of the Work.

        - Verify that finishes of substrates comply with tolerances and other requirements specified in other Sections and that substrates are free of cracks, ridges, depressions, scale, and foreign deposits that might interfere with adhesion of floor coverings.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

      - PREPARATION

Extensive surface preparation is required over substrates from which existing floor coverings have been removed.  Requirements vary among manufacturers.  Insert requirements to suit Project.

        - Prepare substrates according to manufacturer's written instructions to ensure adhesion of floor coverings.

        - Concrete Substrates:  Prepare according to ASTM F 710.

          - Verify that substrates are dry and free of curing compounds, sealers, and hardeners.

          - Remove substrate coatings and other substances that are incompatible with adhesives and that contain soap, wax, oil, or silicone, using mechanical methods recommended by manufacturer.  Do not use solvents.

          - Alkalinity and Adhesion Testing:  Perform tests recommended by manufacturer.  Proceed with installation only after substrates pass testing.

          - Moisture Testing:  Perform tests recommended by manufacturer[ and as follows].  Proceed with installation only after substrates pass testing.

Follow manufacturer's requirements for moisture testing.  Retain one or both subparagraphs below.

            - Perform anhydrous calcium chloride test, ASTM F 1869.  Proceed with installation only after substrates have maximum moisture-vapor-emission rate of [3 lb of water/1000 sq. ft. (1.36 kg of water/92.9 sq. m)] <Insert emission> in 24 hours.

            - Perform relative humidity test using in situ probes, ASTM F 2170.  Proceed with installation only after substrates have a maximum [75 percent] <Insert acceptable percentage> relative humidity level measurement.

        - Fill cracks, holes, and depressions in substrates with trowelable leveling and patching compound and remove bumps and ridges to produce a uniform and smooth substrate.

        - Do not install floor coverings until they are same temperature as space where they are to be installed.

          - Move floor coverings and installation materials into spaces where they will be installed at least 48 hours in advance of installation.

        - Sweep and vacuum clean substrates to be covered by floor coverings immediately before installation.

      - FLOOR COVERING INSTALLATION

        - Comply with manufacturer's written instructions for installing floor coverings.

        - Unroll floor coverings and allow them to stabilize before cutting and fitting.

        - Lay out floor coverings as follows:

          - Maintain uniformity of floor covering direction.

          - Minimize number of seams; place seams in inconspicuous and low-traffic areas, at least 6 inches (152 mm) away from parallel joints in floor covering substrates.

          - Match edges of floor coverings for color shading at seams.

          - Avoid cross seams.

If required, insert requirements for special patterns here.

If built-in items are required to be set on top of floor coverings, indicate on Drawings and revise first paragraph below.

        - Scribe and cut floor coverings to butt neatly and tightly to vertical surfaces, permanent fixtures, and built-in furniture including cabinets, pipes, outlets, and door frames.

        - Extend floor coverings into toe spaces, door reveals, closets, and similar openings.

        - Maintain reference markers, holes, or openings that are in place or marked for future cutting by repeating on floor coverings as marked on substrates.  Use chalk or other nonpermanent marking device.

Retain first paragraph below for floor coverings installed on covers.

        - Install floor coverings on covers for telephone and electrical ducts and similar items in installation areas.  Maintain overall continuity of color and pattern between pieces of floor coverings installed on covers and adjoining floor covering.  Tightly adhere floor covering edges to substrates that abut covers and to cover perimeters.

        - Adhere floor coverings to substrates using a full spread of adhesive applied to substrate to produce a completed installation without open cracks, voids, raising and puckering at joints, telegraphing of adhesive spreader marks, and other surface imperfections.

Retain paragraph below if seamless installation is required.

        - Seamless Installation:

          - Heat-Welded Seams:  Comply with ASTM F 1516.  Rout joints and use welding bead to permanently fuse sections into a seamless floor covering.  Prepare, weld, and finish seams to produce surfaces flush with adjoining floor covering surfaces.

          - Chemically-Bonded Seams:  Bond seams with chemical-bonding compound to permanently fuse sections into a seamless floor covering. Prepare seams and apply compound to produce tightly-fitted seams without gaps, overlays, or excess bonding compound on floor covering surfaces.

        - Integral-Flash-Cove Base:  Cove floor coverings [6 inches (152 mm)] [dimension indicated] <Insert dimension> up vertical surfaces.  Support floor coverings at horizontal and vertical junction by cove strip.  Butt at top against cap strip.

Retain subparagraph below for metal corners.

          - Install metal corners at inside and outside corners.

      - CLEANING AND PROTECTION

        - Comply with manufacturer's written instructions for cleaning and protection of floor coverings.

        - Perform the following operations immediately after completing floor covering installation:

          - Remove adhesive and other blemishes from floor covering surfaces.

          - Sweep and vacuum floor coverings thoroughly.

          - Damp-mop floor coverings to remove marks and soil.

        - Protect floor coverings from mars, marks, indentations, and other damage from construction operations and placement of equipment and fixtures during remainder of construction period.

Before retaining first paragraph below, verify manufacturer's floor polish recommendations.  Floor polish is used with most vinyl sheet floor coverings.

        - Floor Polish:  Remove soil, visible adhesive, and surface blemishes from floor covering before applying liquid floor polish.

Revise subparagraph below to suit products selected.

          - Apply [one] [two] [three] <Insert requirement> coat(s).

        - Cover floor coverings until Substantial Completion.

END OF SECTION 09 65 16