Copyright 2010 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 10 11 00 - VISUAL DISPLAY SURFACES

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

      - RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY

        - Section Includes:

          - Markerboards.

          - Tackboards.

Retain first subparagraph below for display rails that are installed as a separate product; delete if display rails are accessory to chalkboards and markerboards only.

Retain Sections in subparagraphs below that contain requirements Contractor might expect to find in this Section but are specified in other Sections.

      - DEFINITIONS

Retain definition(s) remaining after this Section has been edited.

        - Tackboard:  Framed or unframed, tackable, visual display board assembly.

        - Visual Display Board Assembly:  Visual display surface that is factory fabricated into composite panel form, either with or without a perimeter frame; includes markerboards, and tackboards.

      - ACTION SUBMITTALS

        - Product Data:  For each type of product indicated.  Include construction details, material descriptions, dimensions of individual components and profiles, and finishes for visual display surfaces.

"Product Data for Credit IEQ 4.1" Subparagraph below applies to LEED-NC LEED-CI, and LEED-CS; coordinate with requirements selected in Part 2 for adhesives.

"Product Data for Credit IEQ 4.4" Subparagraph below applies to LEED-NC, LEED-CI, and LEED-CS.

"Laboratory Test Reports for Credit IEQ 4" Subparagraph below applies to LEED for Schools.

        - Shop Drawings:  For visual display surfaces.  Include plans, elevations, sections, details, and attachments to other work.

          - Show locations of panel joints.

          - Include sections of typical trim members.

Retain subparagraph below if equipment includes wiring.

        - Samples for Initial Selection:  For each type of visual display surface indicated, for units with factory-applied color finishes, and as follows:

          - Actual sections of porcelain-enamel face sheet    tackboard assembly   .

          - Fabric swatches of   polyester-fabric-faced tack assemblies.

          - Include accessory Samples to verify color selected.

Delete "Samples for Initial Selection" Paragraph above if colors and other characteristics are preselected and specified or scheduled.  Retain first paragraph below with or without above.

        - Samples for Verification:  For each type of visual display surface indicated.

          - Visual Display Surface:  Not less than 8-1/2 by 11 inches (215 by 280 mm), mounted on substrate indicated for final Work.  Include one panel for each type, color, and texture required.

          - Trim:  6-inch- (152-mm-) long sections of each trim profile.

          - Display Rail:  6-inch- (152-mm-) long sections.

          - Support System:  6-inch- (152-mm-) long sections.

          - Accessories:  Full-size Sample of each type of accessory.

        - Product Schedule:  For visual display surfaces.  Use same designations indicated on Drawings.

      - INFORMATIONAL SUBMITTALS

Retain first paragraph below with qualification requirements in Section 014000 "Quality Requirements."

        - Qualification Data:  For qualified Installer.

        - Product Test Reports:  Based on evaluation of comprehensive tests performed by a qualified testing agency, for surface-burning characteristics of fabrics.

        - Warranties:  Sample of special warranties.

      - CLOSEOUT SUBMITTALS

        - Maintenance Data:  For visual display surfaces to include in maintenance manuals.

      - QUALITY ASSURANCE

Retain first paragraph below if an experienced installer is required for motor-operated, sliding visual display units.

Revise first paragraph below to allow multiple sources for each type of visual display unit.

        - Source Limitations:  Obtain visual display surfaces from single source from single manufacturer.

Retain first paragraph below if testing for surface-burning characteristics is required for product components specified in Part 2.

        - Surface-Burning Characteristics:  As determined by testing identical products according to ASTM E 84 by a qualified testing agency.  Identify products with appropriate markings of applicable testing agency.

          - Flame-Spread Index:  25  or less.

          - Smoke-Developed Index:   450  or less.

Retain first paragraph below if power-operated, visual display surfaces are included.

        - Mockups:  Build mockups to verify selections made under sample submittals and to demonstrate appearance and aesthetic effects and set quality standards for installation.

Retain first subparagraph below for large-scale mockup.  Mockups may be especially prudent for visual display wall panels and wall coverings.  Indicate portion of wall represented by mockup on Drawings or draw mockup as separate element.

          - Build mockup of typical  Visual Display Board Assembly as shown on Drawings.  Include accessories.

Retain subparagraph below if mockups are installed as part of building rather than erected separately and the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups when directed unless otherwise indicated.

          - Approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

Retain paragraph below if Work of this Section is extensive or complex enough to justify a preinstallation conference.

      - DELIVERY, STORAGE, AND HANDLING

Revise first paragraph below to suit Project.  Slate chalkboards are primarily field assembled.  Coordinate type of trim with "(Chalkboard) (Markerboard) (and) (Tackboard) Accessories" Article.

        - Deliver factory-built visual display surfaces, including factory-applied trim where indicated, completely assembled in one piece without joints, where possible.  If dimensions exceed maximum manufactured panel size, provide two or more pieces of equal length as acceptable to Architect.  When overall dimensions require delivery in separate units, prefit components at the factory, disassemble for delivery, and make final joints at the site.

        - Store visual display surfaces vertically with packing materials between each unit.

      - PROJECT CONDITIONS

        - Environmental Limitations:  Do not deliver or install visual display surfaces until spaces are enclosed and weathertight, wet work in spaces is complete and dry, work above ceilings is complete, and temporary HVAC system is operating and maintaining ambient temperature and humidity conditions at occupancy levels during the remainder of the construction period.

Retain paragraph below if natural-slate chalkboards are included or if close tolerances are anticipated.

      - WARRANTY

When warranties are required, verify with Owner's counsel that special warranties stated in this article are not less than remedies available to Owner under prevailing local laws.

Retain first paragraph below for chalkboards and markerboards fabricated with porcelain-enamel face sheets.  Most manufacturers' warranties only include replacement of material; labor for removal and reinstallation is excluded.

        - Special Warranty for Porcelain-Enamel Face Sheets:  Manufacturer's standard form in which manufacturer agrees to repair or replace porcelain-enamel face sheets that fail in materials or workmanship within specified warranty period.

          - Failures include, but are not limited to, the following:

            - Surfaces lose original writing and erasing qualities.

            - Surfaces exhibit crazing, cracking, or flaking.

Retain one of two subparagraphs below.  Verify available warranties and warranty periods with manufacturers listed in Part 2 articles.

          - Warranty Period:  Life of the building.

Some manufacturers also offer warranties for painted-finish chalkboards and tackboards.  See Evaluations.

Verify available warranties and warranty periods for units and components with manufacturers listed in Part 2 articles.

          - Warranty Period:  Two  years from date of Substantial Completion.

Consider inserting warranty provision for motors if motor-operated, sliding visual display units are required.

- PRODUCTS

      - MATERIALS, GENERAL

Porcelain-enamel face sheets are used for chalkboard and markerboard assemblies, wall panels, sliding visual display units, and visual display conference units.  Retain one of first two paragraphs below or delete both and retain third paragraph.  First paragraph is for products by PolyVision Corporation, second is for products by Claridge Products and Equipment, and third is for manufacturer's standard manufacturing method.  See Evaluations.

If needed, insert performance requirements for gloss, surface distortion, light reflectance, impact resistance, etc., of each face sheet.

        - Porcelain-Enamel Face Sheet:  Manufacturer's standard steel sheet with porcelain-enamel coating fused to steel; uncoated thickness indicated.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers.  Retain first subparagraph and list of manufacturers below.  See Section 016000 "Product Requirements."

          - Gloss Finish:  Gloss as indicated; dry-erase markers wipe clean with dry cloth or standard eraser.

Verify availability of product components tested for surface-burning characteristics in first four paragraphs below.  If testing of entire assemblies is required by authorities having jurisdiction, add this requirement to the Section Text.

        - Polyester Fabric:  Nondirectional weave, 100 percent polyester; weighing not less than 15 oz./sq. yd. (508 g/sq. m); with surface-burning characteristics indicated.

Revise first three paragraphs below if product components tested for surface-burning characteristics are required to suit Project.  Verify availability with manufacturers.

        - Hardboard:  ANSI A135.4, tempered.

Retain second option in "Particleboard" Paragraph below if required for LEED-NC, LEED-CI, or LEED-CS Credit IEQ 4.4.  Retain third option if required for LEED for Schools Credit IEQ 4.

        - Particleboard:  ANSI A208.1, Grade M-1, that complies with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

        - Fiberboard:  ASTM C 208.

        - Extruded Aluminum:  ASTM B 221 (ASTM B 221M), Alloy 6063.

Retain "Adhesives" Paragraph below if required for LEED for Schools Credit IEQ 4.

        - Adhesives:  Manufacturer's standard product that complies with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

      - MARKERBOARD ASSEMBLIES

First two options in first paragraph below are for porcelain-enamel face sheet by PolyVision.  Delete both if retaining only porcelain-enamel face sheet by Claridge in "Materials, General" Article.

        - Porcelain-Enamel Markerboards:  Balanced, high-pressure, factory-laminated markerboard assembly of three-ply construction consisting of backing sheet, core material, and 0.021-inch- (0.53-mm-) thick, porcelain-enamel face sheet with high-gloss finish.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers.  Retain first subparagraph and list of manufacturers below.  See Section 016000 "Product Requirements."

          - Basis of Design Product:  Subject to compliance with requirements, provide LCS-II, Series 4, Type A, #92 white by Claridge Products & Equipment, Inc., www.claridgeproducts.com, or comparable product by one of the following:

            - A-1 Visual Systems:  Series 100; www.a-1markerboards.com.

            - Best-Rite Manufacturing:  Series 202A; www.moorecoinc.com.

            - Substitutions:  See Section 01 25 00 - Substitution Procedures.

Retain one of first four subparagraphs below.  Verify availability and thickness with manufacturers selected.  Particleboard core is most dimensionally stable core material listed.

h are intended for dry erasing of chalk and dry-erase markers and for damp-cloth erasing of permanent markers, pens, and pencils.  Users often experience problems with these assemblies.  See Evaluations.

      - TACKBOARD ASSEMBLIES

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers.  Retain first paragraph and list of manufacturers below.  See Section 016000 "Product Requirements."

        - Basis of Design Product:  Subject to compliance with requirements, provide Designer Fabric, Series 4, Type CO, Color to be selected from Manufacturer's standard colors, by Claridge Products & Equipment, Inc. Harrison, Arkansas 72602; www.claridgeproducts.com, or comparable product by one of the following:

          - A-1 Visual Systems:  Series 100; www.a-1markerboards.com.

          - Best-Rite Manufacturing:  Series 333A; www.moorecoinc.com.

          - Substitutions:  See Section 01 25 00 - Substitution Procedures.

Retain types of tackboard assemblies below to suit Project.  See Evaluations.  A few manufacturers also offer tackboard assemblies with a 7/16-inch- (11-mm-) thick fiberboard backing.  Verify availability with manufacturers.

Insert number to complete designation for each assembly retained below.  Use these designations in the "Visual Display Surface Schedule" Article to show where each tackboard is required.

Only a few manufacturers offer assemblies with no backing.

Natural cork is also available with large cork particles fused and compressed into sheets.

        - Polyester-Fabric-Faced Tackboard :  1/4-inch- (6-mm-) thick, polyester-fabric-faced cork sheet factory laminated to 1/4-inch- (6-mm-) thick hardboard  backing.

        - General:  Manufacturer's standard, aluminum-framed, tackable cork  visual display surface fabricated into narrow rail shape and designed for displaying material.

      - MARKERBOARD AND TACKBOARD ACCESSORIES

Retain one or more accessories in this article to suit Project and coordinate with those required in the "Visual Display Surface Schedule" Article.

        - Aluminum Frames and Trim:  Fabricated from not less than 0.062-inch- (1.57-mm-) thick, extruded aluminum;  slim size and standard shape  .

Retain one of two subparagraphs below.

          - Field-Applied Trim:  Manufacturer's standard,   screw-on trim with Phillips flat-head screws.

        - Chalktray:  Manufacturer's standard, continuous.

          - Solid Type:  Extruded aluminum with ribbed section and smoothly curved exposed ends.

Map rails are used at heads of chalkboards, markerboards, and tackboards and as dividers between panels.  Coordinate with information shown on Drawings.  Revise first paragraph below to suit Project.

        - Map Rail:  Provide the following accessories:

          - Display Rail:  Continuous and integral with map rail; fabricated from cork approximately 1 to 2 inches (25 to 50 mm) wide.

Paper holders in subparagraph below can also be applied directly to chalkboards and markerboards rather than to map rails.

      - FABRICATION

        - Porcelain-Enamel Visual Display Assemblies:  Laminate porcelain-enamel face sheet and backing sheet to core material under heat and pressure with manufacturer's standard flexible, waterproof adhesive.

Coordinate first paragraph below with type of trim in "(Chalkboard) (Markerboard) (and) (Tackboard) Accessories" Article.

        - Visual Display Boards:  Factory  assemble visual display boards unless otherwise indicated.

          - Where factory-applied trim is indicated, trim shall be assembled and attached to visual display boards at manufacturer's factory before shipment.

Retain first paragraph below if retaining first option in last paragraph above.

        - Factory-Assembled Visual Display Units:  Coordinate factory-assembled units with trim and accessories indicated.  Join parts with a neat, precision fit.

If locations of joints are critical, show them on Drawings and delete first subparagraph below.

Retain subparagraph below if required.

          - Where size of visual display boards or other conditions require support in addition to normal trim, provide structural supports or modify trim as indicated or as selected by Architect from manufacturer's standard structural support accessories to suit conditions indicated.

        - Modular Visual Display Boards:  Fabricated with integral panel clips attached to core material.

        - Aluminum Frames and Trim:  Fabricate units straight and of single lengths, keeping joints to a minimum.  Miter corners to a neat, hairline closure.

          - Where factory-applied trim is indicated, trim shall be assembled and attached to visual display units at manufacturer's factory before shipment.

      - GENERAL FINISH REQUIREMENTS

        - Comply with NAAMM's "Metal Finishes Manual for Architectural and Metal Products" for recommendations for applying and designating finishes.

        - Protect mechanical finishes on exposed surfaces from damage by applying a strippable, temporary protective covering before shipping.

        - Appearance of Finished Work:  Noticeable variations in same piece are not acceptable.  Variations in appearance of adjoining components are acceptable if they are within the range of approved Samples and are assembled or installed to minimize contrast.

      - ALUMINUM FINISHES

Retain finishes in this article to suit Project.  If retaining more than one, indicate location of each on Drawings or by inserts.

        - Clear Anodic Finish:  AAMA 611, AA-M12C22A31, Class II, 0.010 mm or thicker.

Paragraph below references AAMA standard for pigmented organic coating on extrusions and panels.

      - VISUAL DISPLAY SURFACE SCHEDULE

Retain schedule if required; add any relevant requirements to appropriate article in Part 2 or show on Drawings.

Copy paragraphs below and re-edit for each product.

Insert number to complete drawing designation for each product required.  Use these designations on Drawings to identify each product.

        - Visual Display Board <Insert drawing designation>:  Factory  assembled.

          - Markerboard:  Porcelain-enamel   markerboard assembly.

            - Color:  White     .

          - Corners:  Square .

          - Width:  As indicated on Drawings .

          - Height:  As indicated on Drawings .

          - Mounting:  Wall .

          - Mounting Height:  As indicated on Drawings .

Retain one of three trim subparagraphs below.  Vinyl trim is available only for markerboards.

          - Factory -Applied Aluminum Trim:  Manufacturer's standard  with clear anodic    finish.

Retain one color from options in first subparagraph below with color anodic or finish coat above.  First four options are for color anodic finish and may vary in color range and availability among manufacturers.  Last three options are for color anodic, baked-enamel, or powder-coat finish.

          - Accessories:

            - Chalktray:  Box  type.

            - Map rail with display rail     .

        - Tackboard <Insert drawing designation>:  Factory  assembled.

          - Tack Surface:  Polyester-fabric-faced tackboard assembly <Insert designation>.

Retain first subparagraph below if not retaining natural-cork tackboard assembly above.

            - Color:   Match Architect's sample .

          - Corners:  Square .

          - Width:  As indicated on Drawings .

          - Height:  As indicated on Drawings .

          - Mounting:  Wall .

          - Mounting Height:  As indicated on Drawings .

          - Edges:  Concealed by trim .

Retain one of two trim subparagraphs below.

            - Factory -Applied Aluminum Trim:  Manufacturer's standard  style, with clear anodic    finish.

Retain one color from options in first subparagraph below with color anodic or finish coat above.  First four options are for color anodic finish and may vary in color range and availability among manufacturers.  Last three options are for color anodic, baked-enamel, or powder-coat finish.

        - Visual Display Rail <Insert drawing designation>:  Factory  assembled.

          - Tack Surface:  Polyester-fabric-faced tackboard assembly <Insert designation>.

Retain first subparagraph below if retaining plastic-impregnated-cork, vinyl-fabric-faced, or polyester-fabric-faced tackboard assembly above.

            - Color:   Match Architect's sample .

          - Size:  1 inch (25 mm)   high by length indicated on Drawings.

          - Edges:  Extruded-aluminum trim .

          - Ends:   Not required.

Manufacturers' standard is clear anodic finish.  Verify availability of other finishes with manufacturers and add color if required.

          - Aluminum Finish:  Clear anodic  finish.

Visual display wall panels in first paragraph below are assembled in the field and consist of multiple panels that cover an extensive amount of wall surface.

- EXECUTION

      - EXAMINATION

        - Examine substrates and conditions, with Installer present, for compliance with requirements for installation tolerances, surface conditions of wall, and other conditions affecting performance of the Work.

        - Examine walls and partitions for proper preparation and backing for visual display surfaces.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

      - PREPARATION

        - Comply with manufacturer's written instructions for surface preparation.

        - Clean substrates of substances that could impair the performance of and affect the smooth, finished surfaces of visual display boards, including dirt, mold, and mildew.

        - Prepare surfaces to achieve a smooth, dry, clean surface free of flaking, unsound coatings, cracks, defects, projections, depressions, and substances that will impair bond between visual display surfaces and wall surfaces.

Delete first subparagraph below if priming of surfaces to receive direct-applied, visual display tack wall panels and visual display wall coverings is performed in another Section.

Retain one of two subparagraphs below for visual display wall coverings.

Delete first subparagraph below if priming of gypsum-board surfaces is performed in another Section.

      - INSTALLATION, GENERAL

        - General:  Install visual display surfaces in locations and at mounting heights indicated on Drawings. Keep perimeter lines straight, level, and plumb.  Provide grounds, clips, backing materials, adhesives, brackets, anchors, trim, and accessories necessary for complete installation.

Verify mounting heights required; mounting heights in subparagraphs below are common.  PolyVision recommends mounting heights of 24 inches (610 mm) for kindergarten; 26 inches (660 mm) for Grades 1 through 3; 30 inches (762 mm) for Grades 4 through 6; 34 inches (864 mm) for Grades 7 through 9; and 37 inches (940 mm) for Grades 10 and higher.

      - INSTALLATION OF FACTORY-FABRICATED VISUAL DISPLAY BOARDS AND ASSEMBLIES

Retain one of two paragraphs below or revise to suit product and Project.

        - Visual Display Boards:  Attach concealed clips, hangers, and grounds to wall surfaces and to visual display boards with fasteners at not more than 16 inches (400 mm) o.c.  Secure both top and bottom of boards to walls.

Retain one of two subparagraphs below with either paragraph above.

          - Field-Applied Aluminum Trim:  Attach trim over edges of visual display boards and conceal grounds and clips.  Attach trim to boards with fasteners at not more than 24 inches (610 mm) o.c.

            - Attach chalktrays to boards with fasteners at not more than 12 inches (300 mm) o.c.

      - INSTALLATION OF VISUAL DISPLAY RAILS

        - Display Rails:  Install rails in locations and at mounting heights indicated on Drawings.  Attach to wall surface with fasteners at not more than 16 inches (400 mm) o.c.

      - INSTALLATION OF VISUAL DISPLAY WALL PANELS

      - INSTALLATION OF [RAIL] [MODULAR] SUPPORT SYSTEM

        - Rail Support System:  Install horizontal support rail in locations and at mounting heights indicated on Drawings, or if not indicated, at height indicated below.  Attach to wall surface with fasteners at 12 inches (300 mm) o.c.

          - Mounting Height:  [72 inches (1829 mm)] <Insert dimension> above finished floor to top of rail.

          - Hang visual display units on rail support system.

        - Modular Support System:  Install adjustable standards in locations and at mounting heights indicated on Drawings, or if not indicated, at height indicated below.  Install standards at 48 inches (1219 mm) o.c., vertically aligned and plumb, and attached to wall surface with fasteners at 12 inches (300 mm) o.c.

          - Mounting Height:  [12 inches (300 mm)] <Insert dimension> above finished floor to bottom of standard.

          - Install single-slotted standard at each end of each run of standards and double-slotted standards at intermediate locations.

          - Provide locking screw at top corner of visual display board at each standard.

          - Hang visual display units on modular support system.

      - CLEANING AND PROTECTION

        - Clean visual display surfaces according to manufacturer's written instructions.  Attach one cleaning label to visual display surface in each room.

        - Touch up factory-applied finishes to restore damaged or soiled areas.

        - Cover and protect visual display surfaces after installation and cleaning.

END OF SECTION 10 11 00